## Slide 1: CH2PH2: Surfaces and Interfaces
Dr. James Hallett
j.e.hallett@reading.ac.uk

## Slide 2
CH2PH2
Lecture 4: Liquid Crystals

## Slide 3: What are liquid crystals?
“A state of matter whose properties are between those of a regular
Liquid and a crystalline solid”
What are some properties of liquids and crystalline solids?

## Slide 4: Crystal
(Nematic) Liquid
Crystal
Liquid

## Slide 5: S= 1
S= 0
S ~ 0.6
Order parameter
Where theta is the angle between the molecular axis and the director n
n

## Slide 6
https://youtu.be/HEwGeqR4duQ
Background context

## Slide 7: Second law of thermodynamics
“the total entropy of a system either increases or remains constant in any spontaneous process; it never decreases”

## Slide 8
Excluded volume
Free volume
Although orientational entropy goes down (and free energy goes up) when molecules align in a nematic,
positional entropy increases (so free energy goes down).

## Slide 9: Typical liquid crystal molecules
Typical liquid crystal molecules are:
“rod like”, so they form a nematic phase
have an alkyl tail so they stay liquid at room temperature
have a large dielectric anisotropy (how easy it is to polarise the molecule along the long axis versus the short axis), so they can be reoriented easily by an electric field.
Chemical innovation usually involves improving one of these properties – novel liquid crystal molecules/compositions are closely guarded secrets!
“5CB” - 4-Cyano-4'-pentylbiphenyl
Very good for Raman
Spectroscopy!

## Slide 10: Liquid crystal displays (LCDs)
Background context

## Slide 11: LCDs
Background context

## Slide 12: Pixel size in LCD displays
~336 ppi,
75 μm pixel size
~163 ppi,
153 μm pixel size
Background context

## Slide 13: A simple LC display pixel
Image source: pixelstrobist
-
+
- - -
+ + +

## Slide 14: Crossed polarizers
https://youtu.be/iAILxVfHse0

## Slide 15: Crossed polarizers
https://youtu.be/OQiSXUfeKaQ

## Slide 16: LCDs

## Slide 17: The Frederiks (Fréedericksz) Transition
The voltage required to “switch” the liquid crystal cell from one orientation to another.
Sometimes expressed as a critical electric field (V/d)
Depends on liquid crystal “elasticity” and “dielectric anisotropy” – how hard it is to bend the director to a new direction versus how sensitive it is to electric field
Δ𝜖 – dielectric anisotropy
𝜖0 – permittivity of free space = 8.85 ✕ 10-12 C2 N-1 m-2
Kii – elastic term (varies for different geometries)

## Slide 18: New LC technologies
Shukla, R. K., Chaudhary, A., Bubnov, A., Hamplova, V., & Raina, K. K. (2020). Electrically switchable birefringent self-assembled nanocomposites: ferroelectric liquid crystal doped with the multiwall carbon nanotubes. Liquid Crystals, 47(9), 1379-1389.
Li, X., Zhang, M., Zhang, C., Niu, R., Ma, H., & Sun, Y. (2023). A bistable ion-doped cholesteric liquid crystal smart window with a small amount of polymer. Optical Materials, 138, 113659.
“Bistable” – doesn’t use power to display an image
“Electrochromic” change colour with voltage – no need for colour filters
Background context

## Slide 19
https://www.youtube.com/watch?v=WGcBtN7axYQ
Background context

## Slide 20: Chemical sensors
Carlton, R. J., Hunter, J. T., Miller, D. S., Abbasi, R., Mushenheim, P. C., Tan, L. N., & Abbott, N. L. (2013). Chemical and biological sensing using liquid crystals. Liquid crystals reviews, 1(1), 29-51.
Background context

## Slide 21: Families of liquid crystals
Pure molecular liquids – phase behaviour depends on temperature
Solutions of molecules – phase behaviour also depends on concentration
Thermotropic
Lyotropic
Luders, D. D., Oliveira, D. A., Kimura, N. M., Simões, M., & Palangana, A. J. (2015). Order parameter in the nematic–isotropic phase transition. J. Molecular Liquids, 207, 195-199.
Qiu, H., & Caffrey, M. (2000). The phase diagram of the monoolein/water system: metastability and equilibrium aspects. Biomaterials, 21(3), 223-234.

## Slide 22
Some examples of phase diagrams for non-ionic Surfactants.
Here C denotes a methylene group and E an oxyethylene group.
The dashed lines are approximate phase boundaries and the dot-dash line is the cmc
S=solid phase, W = aqeuous phase (containing unassociated surfactant)
Lyotropic phase diagrams

## Slide 23
Lyotropic liquid crystals
At concentrations well above the cmc, surfactants can form lyotropic liquid crystal phases (and some are even thermotropic liquid crystals).
The phase formed depends on the concentration (hence the term lyotropic) and on the molecular structure.

## Slide 24
Lyotropic liquid crystals
At concentrations well above the cmc, surfactants can form lyotropic liquid crystal phases (and some are even thermotropic liquid crystals).
The phase formed depends on the concentration (hence the term lyotropic), temperature and on the molecular structure.
La
P
D
G
HII
L2

## Slide 25
Inverse phases

## Slide 26: The lamellar phase
Water channel
Lipid bilayer
Water channel
The fluid lamellar phase (L)- can be thought of as a one-dimensional stack of bilayers.
Each bilayer, separated by a region of water is made up of molecules placed back to back producing two parallel planar polar interfaces.
In the L phase movement within the bilayer is not restricted as the alkyl chains are melted and fluid-like.

## Slide 27
Bicontinuous phases
Single continuous bilayer which divides space into two inter-linked but separate aqueous sub-volumes.
Bilayer draped upon IPMSs (Infinite Periodic Minimal Surfaces)

## Slide 28: Biological relevance
Evidence suggesting complex lyotropic structures such as the inverse bicontinuous cubic phases form within cells and perform important biological functions
Membrane fusion and fission must eventually proceed via structural routes that must be closely similar to those which occur during lyotropic phase transitions
This is of central importance to our understanding of endo- and exocytosis
Lamellar phase
Bicontinuous cubic
phase
Studying membrane proteins in bicontinuous
phases is more “realistic” than in solution

## Slide 29: The hexagonal phase
The hexagonal phase can be visualised as a set of cylinders packed onto a 2-D hexagonal lattice.
This phase is often formed by lipids such as phosphatidylethanolamine (PE) which are present in high concentrations in cellular systems.
In the HII phase cylinders of water (typically 10-20 Å in diameter) are surrounded by amphiphiles with lattice dimensions of the order of 50 to 90 Å
Implicated in membrane fusion

## Slide 30
A high-surface-area “mesoporous” material can be used in applications like catalysis and separations – pore size targets specific molecules
Templated lyotropic phases

## Slide 31
Mechanisms of formation for “mesoporous” MCM-41 silica. Offers tunable pore size for targeting different molecules and widely used in catalysis, catalyst supports and separations
Templated lyotropic phases

## Slide 32
Templated lyotropic phases
Wilts, B. D., Apeleo Zubiri, B., Klatt, M. A., Butz, B., Fischer, M. G., Kelly, S. T., ... & Schröder-Turk, G. E. (2017). Butterfly gyroid nanostructures as a time-frozen glimpse of intracellular membrane development. Science advances, 3(4), e1603119.
Background context

## Slide 33
The phase behaviour of amphiphiles can be rationalised on the basis of interfacial curvature.
This can be analysed using differential geometry (assuming a continuous surfactant “film” Or
on a molecular basis – molecular packing parameter model
Structure formed depends on the relative size of the hydrophobic tail and hydrophilic head-group.
The area per head group depends on the extent of hydration and therefore we refer to effective area per Headgroup.
Lyotropic liquid crystals

## Slide 34
We now define a packing parameter, Ns.
Consider the micellar association number, p.
For a spherical micelle, It can be written as the ratio of the micelle volume to the volume per molecule
The association number can similarly be calculated from the ratio of micellar area to the effective area per headgroup, a:
Equating the two expressions for p:
Since r cannot exceed the length of a fully extended chain, l
LHS is the surfactant packing parameter
Lyotropic liquid crystals

## Slide 35
The packing parameter depends on concentration, reflecting changes primarily in a, but also in V.
A similar calculation to that for spherical micelles, leads to the following sequences of inequalities for different aggregate shapes:
Lyotropic liquid crystals

## Slide 36
Lyotropic liquid crystals
La
P
D
G
HII
L2
Increasing negative curvature

## Slide 37: Learning Outcomes
Today we have: Understood the switching mechanism of liquid crystal displays Described the different phase behaviour of thermotropic and lyotropic liquid crystals Related the molecular packing parameter to different lyotropic liquid crystal phases.

## Slide 38
Summary:
Surface and interfacial tension
Surfactancy
Gibbs adsorption isotherms
Micellization and surface activity
Critical micelle concentration as equilibrium
Thermodynamics of micellization
Liquid crystal phases